SECTION 08360

SECTIONAL OVERHEAD DOORS

MODEL 3550 ALUMINUM FULL VIEW

Display hidden notes to specifier by using “Tools”/”Options”/“View”/”Hidden Text” in MS Word 2003 or “Word Options”/”Display”/Hidden Text” in MS Word 2007, or “File” / ”Options” / ”Display/ ”Hidden Text” in MS Word 2010 .

** NOTE TO SPECIFIER **  Amarr Garage Door commercial insulated, non-insulated and aluminum sectional overhead door products.

.

This section is based on the products of Amarr Garage Door, which is located at:

165 Carriage Court

Winston-Salem, NC 27105

Tel: (800) 503-3667

Fax: (336) 251-1851

Email: marketing@amarr.com

www.amarr.com

[click Here] for additional information.

Amarr Garage Doors has been known and respected for its standard of excellence since 1951. Careful attention to detail, the highest quality construction, and unique features are built into every Amarr door. Regardless of model or style, you can be confident that the Amarr door you choose is the finest available and will provide the utmost in security, beauty and value.

Amarr has 69 Door Centers spread throughout the United States, Canada, and Mexico. Each of these Amarr Garage Door Centers are “mini-plants”, stocked with hundreds of sizes and styles of commercial and residential garage doors. In addition, because sometimes you need a door fast, each Door Center can customize doors with options and accessories, to fit most openings – usually within 24 hours.

Amarr Door Centers are staffed with managers who can help you with your day-to-day questions about garage doors, track and springing specifications. This local manager is a reliable source of information for you…when you need it.

Amarr Garage Doors are installed throughout the United States, Canada, and Mexico by professional garage door installers. For the Amarr Door Center nearest you, call our toll free number. We will be happy to direct you to a reliable Amarr Dealer in your area.

SECTION 08360 – SECTIONAL OVERHEAD DOORS

GENERAL

SECTION INCLUDES

** NOTE TO SPECIFIER **  Delete items below not required for project.

Aluminum Doors

Track and Framing

RELATED SECTIONS

** NOTE TO SPECIFIER **  Delete any sections below not relevant to this project; add others as required.

Section 04810 - Unit Masonry Assemblies: Prepared opening in masonry.

Section 05500 – Metal Fabrications: - Steel framed door openings.

Section 06100 – Rough Carpentry: Wood framing and blocking for door opening.

Section 07900 - Joint Sealers: Perimeter sealant and backup materials.

Section 08710 - Door Hardware: Cylinder locks.

REFERENCES

** NOTE TO SPECIFIER **  Delete references from the list below that are not actually required by the text of the edited section.

ASTM A 653/A 653M – Specification for Steel Sheet, Zinc-Coated (Galvanized) or Zinc-Iron Alloy-Coated (Galvannealed) by the Hot-Dip Process.

ASTM B 209/209M – Specification for Aluminum and Aluminum-Alloy Sheet and Plate.

ASTM B 221/221M – Specification for Aluminum and Aluminum-Alloy Extruded Bars, Rods, Wire, Profiles and Tubes.

ANSI/DASMA 102-1996.

SUBMITTALS

Submit under provisions of Section 01300.

Product Data:  Manufacturer's data sheets on each product to be used, including:

Preparation instructions and recommendations.

Storage and handling requirements and recommendations.

Installation methods.

Operation and maintenance data.

Shop Drawings: Include opening dimensions and required tolerances, connection details, anchorage spacing, hardware locations, and installation details.

** NOTE TO SPECIFIER **  Delete selection samples if colors have already been selected.

Selection Samples:  For each finish product specified, two complete sets of color chips representing manufacturer's full range of available colors and patterns.

Verification Samples:  For each finish product specified, two samples, minimum size 6 inches (150 mm) square, representing actual product, color, and patterns.

WIND PERFORMANCE REQUIREMENTS

Design doors to withstand positive and negative wind loads as calculated in accordance with applicable governing building codes.

QUALITY ASSURANCE

Manufacturer Qualifications: Company specializing in manufacturing the types of doors specified in this section with minimum five years documented experience.

Installer Qualifications: Installation to be by qualified dealer in accordance with the manufacturer’s installation instructions.

DELIVERY, STORAGE, AND HANDLING

Store products in manufacturer's unopened packaging until ready for installation.

PROJECT CONDITIONS

Maintain environmental conditions (temperature, humidity, and ventilation) within limits recommended by manufacturer for optimum results.  Do not install products under environmental conditions outside manufacturer's absolute limits.

WARRANTY

1-year limited warranty on materials and workmanship.

5-year limited warranty on finish.

PRODUCTS

MANUFACTURERS

Acceptable Manufacturer:  Amarr Garage Doors; 165 Carriage Court, Winston-Salem, NC  27105.  ASD. Tel: (800) 503-3667.  Fax: (336) 251-1851.  Email: marketing@amarr.com Website: www.amarr.com.

** NOTE TO SPECIFIER **  Delete one of the following two paragraphs; coordinate with requirements of Division 1 section on product options and substitutions.

Substitutions:  Not permitted.

Requests for substitutions will be considered in accordance with provisions of Section 01600.

OVERHEAD DOORS - GENERAL

Provide each door with door sections, brackets, tracks, counterbalance mechanisms and hardware to suit the opening and headroom available.

Hardware:

Minimum of 14 gauge galvanized steel hinges and 13 gauge galvanized steel track brackets.

Rollers have 10 ball bearings with casehardened inner and outer races.

Sliding end stile locking device provided with spring-loaded bolt for inside operation only.

Doors 16 feet 4 inches (5102 mm) and wider provided with double end hinges and stiles and long stem rollers.

Tracks: 2 inches (51 mm) or 3 inches (76 mm) as required.

Vertical track 17 or 19-gauge minimum galvanized steel, inclined using adjustable brackets to assure weather tight closure at the jambs.

Horizontal tracks 16-gauge minimum galvanized steel, reinforced with 13 gauge galvanized steel angles as required by door size and weight.

** NOTE TO SPECIFIER **  Select from the following track options; delete options not used.

Provide vertical lift tracks as indicated.

Provide high lift tracks as indicated.

Provide follow roof slope tracks as indicated.

Provide low headroom tracks as indicated.

Spring Counterbalance: Torsion springs for door counter-balance mounted on a continuous cross header shaft. Springs to be oil tempered, helical wound and custom computed for each door. Cable drums to be die cast aluminum. Galvanized lift cable to provide minimum safety factor of five to one. Springs to comply with ANSI/DASMA 102-1996 as follows:

** NOTE TO SPECIFIER **  Select from the following spring cycle options; delete options not used.

Standard Cycle Spring: 10,000 cycles.

High Cycle Spring: 25,000 cycles.

High Cycle Spring: 50,000 cycles.

High Cycle Spring: 100,000 cycles.

Handle: Galvanized steel step plate/lift handle provided on inside and outside of bottom section.

Lock: Standard interior sliding end stile lock with hole to receive padlock.

** NOTE TO SPECIFIER **  Select one of the following mounting conditions; delete other.

Mounting: Continuous reverse angle mounting for steel jambs.

Mounting: Bracket mounting for wood jambs.

ALUMINUM DOORS

** NOTE TO SPECIFIER **  Select one of the following models; delete other.

Model 3550HD commercial aluminum full-view door.

Door Size: As indicated on the Drawings.

Door Sections: 2 inches (51 mm) thick. Rails and stiles extruded from 6063-T5 aluminum to produce a door thickness of 2 inches (51 mm). Center stiles to be 2-3/4 inches (70 mm). End stiles to be 3-3/8 inches (86 mm). Top rails to be 3-7/8 inches (98 mm) or 1-15/16 inches (39 mm). Intermediate rails to be 3-3/4 inches (95 mm) per pair. Bottom rails to be 3-7/8 inches (98 mm). All stiles and rails to be secured with 5/16 inch (8 mm) diameter through rods.

** NOTE TO SPECIFIER **  Select from the following color options; delete options not used.

Door Finish:

All aluminum rails and stiles to be a clear anodized finish.

All aluminum rails and stiles to be a dark bronze anodized finish.

All aluminum rails and stiles to be a black anodized finish.

All aluminum rails and stiles to be a white powder coat finish.

All aluminum rails and stiles to be a custom (Specifier to add RAL number and description here) powder coat finish.

** NOTE TO SPECIFIER **  Select from the following panel options; delete options not used.

Solid Panels: 0.050 inch (1.3 mm) aluminum panels in continuous gasket and held in place with an aluminum bead.

Glazed Panels: 1/8 inch (3.2 mm) DSB glass panels in a continuous gasket and held in place with an aluminum bead.

Glazed Panels: 1/8 inch (3.2 mm) Tempered glass panels in continuous gasket and held in place with an aluminum bead.

Glazed Panels: 1/2 inch (12.7 mm) overall insulated double pane 1/8” (3.2 mm) DSB glass panels in continuous gasket and held in place with an aluminum bead.

Glazed Panels: 1/2 inch (12.7 mm) overall insulated double pane 1/8” (3.2 mm) Tempered glass panels in continuous gasket and held in place with an aluminum bead.

FABRICATION

** NOTE TO SPECIFIER **  Select one of the following models; delete other.

Aluminum Doors.

3550 standard maximum size: 24 feet 2 inches wide by 18 feet 1 inch high (7.4m by 4.9m). for doors with aluminum or 1/8” glass panels. 20 feet 2 inches wide by 18 feet 1 inch high (6.2m by 4.9m) for doors with 1/2" insulated double pane glass panels.

Aluminum struts (truss bars): Provide struts that do not block the viewable area of glazed panels on all 3550 doors 16 feet 4 inches (5.0m) and wider to prevent deflection of no more than 1/120 of the spanned width when in the open position.

EXECUTION

EXAMINATION

Do not begin installation until substrates have been properly prepared.

Verify wall openings are ready to receive work and opening dimensions and tolerances are within specified limits.

PREPARATION

Clean surfaces thoroughly prior to installation.

Prepare opening to permit correct installation of door unit to perimeter air and vapor barrier seal.

INSTALLATION

Install in accordance with manufacturer's instructions. Doors to be interior face mounted on a prepared surface.

Anchor assembly to wall construction and building framing without distortion.

Securely brace door tracks suspended from structure. Secure tracks to structural members or solid backing only.

Fit and align door assembly, tracks and operating hardware.

Install perimeter weatherstripping.

Adjust door assembly to smooth operation and in full contact with weatherstripping.

CLEANING

Clean doors, frames and glass.

Remove labels and visible markings.

PROTECTION

Protect installed products until completion of project.

Touch-up, repair or replace damaged products before Substantial Completion.

END OF SECTION